HOH Ecotech Decking Installation Introduction

HOHEcotech wpc decking is made of natural wood/bamboo fiber, plastic particles and special chemical additives, and made by professional wpc production equipment with special production process. With the composition of natural fibers, wpc profile has better anti-UV (ultraviolet) performance and lower expansion and contraction properties according to the change of temperature, and is easy to process as wood. WPC outdoor decking has been widely used resently because of its low moisture absorption, slip resistance rot resistance, termite and other insects resistance, comparative color stability, no-deformed, almost no cracks, no maintenance, etc.

No need of painting or glue, wpc is a kind of environmental-friendly material better for human health. The main ingredient in natural wood/bamboo powder of wpc is the leftover material of furniture or decking factories, while the other main raw material of plastic is recycled plastic. Therefore wpc products is environment-friendly, low-carbon high-tech product advocated by people all over the world for using wpc can save a lot of natural wood and reduce the widespread use of plastic products. .

Our company passed ISO9001: 2008 and ISO14001: 2004 system certification, and do strict control in raw material purchase and production process in order to

ensure quality to meet demand customers. The natural wood/bamboo powder we purchased also comes from professional wood/bamboo powder manufacturers, besides, the plastic we use is Grade A plastic comes from designated domestic manufacturers.

I. Announcements before installation

We suggested that Installation should be done by professional staff. Before fixing, keep the ground dry, clean and smooth. If has local special rules for structure, please follow the rules.

The decking boards are especially for decking. It’s forbidden to put to other uses, like: construct support, connector, or to be some parts of other load-bearing.

Our company will not take the responsibility of the result if the installation does not follow the installation instructions.

II. Installation tools

Electric drill is a necessary tool during installation. For the brittle feature of WPC, pre-drilling should be done, and then fasten screw. Do not fasten screw directly, the WPC materials might be damaged.

Reciprocating drill is also important during the joist-installation. First using the reciprocating drill to drill a hole in the ground, then fasten the plastic expansion pipe. Finally fasten crews.

In the installation, ordinary engineering tools are essential. In the process, suggest wearing thick gloves. We also recommend stainless steel crews of our company for fastening. Ever square meter need about 24pcs screws. However in the practical applications, it’s no need to use them all according to the practical condition.

III．About the WPC attributes

The moisture absorption rate of WPC materials is 0.2%, while expansion rate is around 0.5%. So during the installation, need to calculate the necessary interspaces according to the length and width.

Keep the decking smooth, if have to install the decking boards at some active place, do not fixed too tight.

In order to avoid the surface ponding, the groundwork needs to be slightly lean.

IV. Main accessories Decking:

WPC joist: (Cross dimensions) 40mm（W）×30mm(H) ×Length

stainless steel screw	stainless steel clip	stainless steel clip	stainless steel clip

(use with joist)

T-plastic clip	7-style end cover	end cover	Stainless steel clip

V. Installation Steps

Step 1: fixing the deck to the joist

Before fixing the joist, make sure the ground are clean and smooth. Pave the joist on the ground with a spacing distance of 30cm(suggest distance).At the layup, left a distance of 5mm for expansion(Figure 2). According to different installation condition, offer several fixing methods for your choice, see as blow:

- Electric-drill: Drill a pre-hole in the joist which should be little smaller than the stainless steel screws; Percussion drill: Drill a pre-hole in the ground, then screw the plastic expansion tube; Final, fixing the joist with crews to the ground. The crews must be all put into the joist, or else might bring about the unfairness of the surface(Figure 1).

- No need of the screw. Fix joist to the flat ground with glue, then filled with the cement on the space—more than half of the height—between joists. When the cement solidification, come to next step.

- Use stainless steel joist clip, which is corner brace, each joist 3 clips per meter. Pre-drill with a drill-bit on the ground, and put the plastic expansion cover into it, then fix the corner brace on the ground by screws. Better to use the cement to cover both sides of each joist.

Comparatively the third method is the best—effective and economical. (Figure 3)

Step 2: Fix decking onto joist

When install the first piece of the decking, fix HP-4 accessory on the joist, then insert the joist. Plastic clip or stainless steel clip must be taked to fix boards. After fixing two boards, push the board by edge so that the slots between the boards fix well,and finally screw the nail in the middle of the plastic clip.

Note: Please arrange more than two workers during installation, since the material would be possiblly damaged if hit by heavy things or fall from high place.

VI. Usage & Clean

| SN | Possible Problem | Solution |
| --- | --- | --- |