**4629079HANGZHOU FOREVER PLASTICS CO., LTD**

**4629076**3680087 **NO.278,QINGXIAN ROAD,LINGLONG STREET,LINAN,HANGZHOU,ZHEJIANG,CHINA.**

**: 86-15700086631 : 0086-571-63700112 www.foreverseal.cn**

**PINK PLUMBER LINE THREAD SEAL TAPE**

Pink Plumber Line Thread Seal Tape is a full density thread seal tape for used with piping in air,water,sewage,hydraulic lines and sprinkler systems.

PHYSICAL PROPERTIES:

Thickness: 0.1mm/0.004’’

Width: 12mm(1/2”) 19mm(3/4”) 25mm(1”)

Density: 1.20g/cm3 to 1.50g/cm3

Composition: Min. 99% virgin PTFE, Max. 1% pigment



Temp.Range: -450F to +500F (260)

Pressure Rating: up to10,000PSI

Tensile Strength: 15N/mm2

Elongation: Min 50%

Storage: Unlimited shelf life (less than 70F recommended)

Flammability: Non-fammable

