|  | Hangzhou Ponray Technologies Co., Ltd Add: Rm1903, Bldg No.1, No.555,Xincheng Rd, Binjiang,Hangzhou, China Zip:310052 Tel: +86-571-86433485 Fax: +86-571-86433481 |
| --- | --- |
|  | www.best-welding-machine.com |
|  | connucwelder@gmail.com |

Automatic Gantry Welding Machine for wire shelf/wire mesh

Part A: Customized Design

Customized application: for the production of refrigerator wire shelf

According to the welding requirement & the dimension of all wire shelves, we designed machine DN-2×150KVA gantry automatic welding machine with double stations, so two shelves can be weld horizontally at the same time, also machine can automaticlaly feed steel wire vertically, it will greatly improve working efficiency.

Therefore the design of this machine is also for reference of any steel wire products including wire shelf, wire mesh, defence guard etc.

Part B: Construction of the machine

The diameter of the steel wire: φ2.5-7mm

Dimension of the grid: the available width is 914mm (the joint of two grids maximum width)

Dimension of the grid: the available length is 720mm (the maximum length of a grid)

PART C:

The general design sketch of machine structure:

Part D: Machine general description:

The machine is consisted of two parts: the working part and the controlling part.

1. The machine is designed with gantry frame, there are two AC resistance welding transformers (150KVA) installed under the machine rack, one working of both transformers can finish the welding of one row steel wire.

2. Machine’s welding part adopts pneumatic system, eight welding cylinders are installed on top of the machine, and each cylinder provides separate welding pressure needed for each welding spot. There are two support cylinders below the machine, they work together when welding.

3. In the front of machine working table, there is sliding device (like trolley) to put steel wire shelf; the welding fixture loaded on the trolley.

4. All performance of the machine is controlled by the PLC (Programmable Logic Controller), there are two resistance welding controllers equipped to control pressurization, welding, maintenance, pause time & welding current.

5. In the rear of the machine, the feeding device is installed; it automatically drops 1 horizontal wire simutaneously.

6. During the welding process, workers only need to put the shelf frame & take out finished shelf from fixture by hand; All other steps including delivering, stepping, welding, feeding, resetting act automatically.

7. Capacity is 2x150KVA, the voltage is 380V±10%, 50/60Hz, the pressure of the compressed air is more than 0.6Mpa, the pressure of the cooling water is more than 0.2Mpa.

Part E: Design advantage:

Controlled by the PLC, the welding performance is normative; it can weld multiple wire shelf products in big Lot.

The machine adopts module of one-time pressing & electric discharging welding, it can reduce the deformation of wire shelf.

It is suitable to any dimension shelf within the sizes, only needs to change the fixture and adjust the feeding device.

The electricity of each cylinder is independent and can be controlled freely in certain range; it is convenient and easy to operate.

One-time pressure welding, save time and improve the production efficiency.

The welding speed: 1~2 seconds/row

The machine is controlled by the microcomputer; it can store mutiple welding parameters for different products.

Part F: The welding process

Put shelf frame on fixture manually—press the switch to start-- the motor delivers the fixture to welding area—the lower cylinder lift, at the same time the material suction device rises—steel wire automatic feeding—welding as setting program—the motor brings fixture to the next working area—repeat above action…the welding finishes—the motor brings fixture to resetting position & worker take out wire shelf from fixture.

Part G: The main parts:

| Part Name | Brand | Origin |
| --- | --- | --- |
| Cylinder, Filter voltage regulator | / | Made in Taiwan |
| Electromagnetc valve | NORGREN | Made in U.K |
| Silicon steel sheet | KAWASAKI | Made in Japan |
| Main controlling board | / | Made in China |
| Servo motor | DELTA | Made in Taiwan |
| Sliding rack | / | Made in Taiwan |
| Programmable logic controller (PLC) | MITSUBISHI | Made in Japan |
| Thyristor | TECHSUM | Made in Taiwan |
| Electrode | Alloy-copper | Made in China |

Part H: Main technical specifications:

The input voltage: 380±10％   50/60Hz

The rated power: 2×150KVA

The secondary voltage: 11V

The max welding current: 28.7KA

The loading duration factor: 50%

Insulation resistance of the input current to the machine body: ≥2.5MΩ

The working environment:temparture≤ 40℃,relative humidity≤90％

The pressure of the air supply: ≥0.5Mpa

The working pressure: adjustable from 0.5 to 2.2KN

The cooling way of the electrode: the cycled water-cooling

The production efficiency: 4~6 shelves/minute

Part I: Delivery time

By 60 working days.

Acutal welding machine produced for customer: