
**PPGI color coated galvanized steel plate in coil JIS standard SGCC grade**



http://img1.cdn.tradew.com/Y201701M1571336T6G6338779/W0H0/.jpg

Product Details

|  |  |
| --- | --- |
| Size | (0.13mm-5.0mm )\*(600mm-1500mm)\*coil |
| Steel Grade | JIS G3302 SGCC~SGC570,SGCH(FULL HARD-G550),SGHC~SGH540  EN 10346-DX51D+Z,DX53D+Z, S250GD~S550GD  ASTM A653M CS-B, SS255~SS550 |
| Coil Weight | 3MT-14MT |
| Coil ID | 508mm/610mm |
| Chemical Treatment | Chromated(Cr 3+,6+,0+) |
| Surface | chromed / skinpass/ oiled/slightly oiled/ dry/ anti-fingerprint |
| Oil | Slight Oiled/Dry |
| Spangle | Regular/Zero/Big |
| Zinc Coating | Z40-Z300 |
| Capacity | 1,500,000MT/year |
| Mill Origin | HBIS-Tangsteel,Shandong Zhongguan, Changshu Everbright, WISCO |

Standard and Grade of HDG steel sheet/coil PPGI/PPGL

|  |  |  |  |
| --- | --- | --- | --- |
| NAME | PPGI | GALVANIZED | GALVALUME/ALUZINC |
| STANDARD | EN10142  JIS G3302  GB/T-12754-2006 | ASTM A653  JIS G3302  SGCC/SGCH  GB/T2518  European Standard | ASTM A792  JIS G3321  JIS G3317 |
| GRADE | CGCC  CGCH  CGCD1-CGCD3  CGC340-CGC570  GRADE | SS GRADE33-80  SGCC  SGCH  SGCD1-SGCD3  SGC340-SGC570  SGCC  DX51D | GRADE33-80  SGLCC  SGLCD  SGLCDD  SGLC400-SGLC570  SZACC  SZACH  SZAC340R |
| MODEL NO | 0.16MM-1.5MM\*1250MM OR UNDER | (0.12-1.5)\*1250MM OR UNDER | 0.16MM-1.5MM\*1250MM OR UNDER |
| TYPE | Steel coil  Steel sheets/plates  Corrugated steel sheets/plates | Steel coil  Steel sheets/plates  Corrugated steel sheets/plates | Steel coil  Steel sheets/plates  Corrugated steel sheets/plates |
| TECHNIQUE | Hot rolled-cold rolled  -galvalume /galvanized  -PPGI/PPGL | Hot rolled-cold rolled  - galvanized | Hot rolled-cold rolled  -galvalume /Aluzinc |
| SURFACE  TREATMENT | Mini/regular/big/zero spangle,  Chromate treatment /chromate-free treatment /untreated unoile/oiled,  TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,  Coating,color | Mini/regular/big/zero spangle,  Chromate treatment /chromate-free treatment /untreated unoile/oiled,  TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,  Coating | |
| APPLICATION | Structural use ,roofing, commercial use, household appliance, industry, family | | |
| SPECIAL  APPLICATION | Wear resistant steel, high- strength - steel plate | | |

http://img1.cdn.tradew.com/Y201701M1571336T6G6338807/W0H0/.jpg

|  |  |  |  |
| --- | --- | --- | --- |
| NAME | PPGI | GALVANIZED | GALVALUME/ALUZINC |
| STANDARD | EN10142  JIS G3302  GB/T-12754-2006 | ASTM A653  JIS G3302  SGCC/SGCH  GB/T2518  European Standard | ASTM A792  JIS G3321  JIS G3317 |
| GRADE | CGCC  CGCH  CGCD1-CGCD3  CGC340-CGC570  GRADE | SS GRADE33-80  SGCC  SGCH  SGCD1-SGCD3  SGC340-SGC570  SGCC  DX51D | GRADE33-80  SGLCC  SGLCD  SGLCDD  SGLC400-SGLC570  SZACC  SZACH  SZAC340R |
| MODEL NO | 0.16MM-1.5MM\*1250MM OR UNDER | (0.12-1.5)\*1250MM OR UNDER | 0.16MM-1.5MM\*1250MM OR UNDER |
| TYPE | Steel coil  Steel sheets/plates  Corrugated steel sheets/plates | Steel coil  Steel sheets/plates  Corrugated steel sheets/plates | Steel coil  Steel sheets/plates  Corrugated steel sheets/plates |
| TECHNIQUE | Hot rolled-cold rolled  -galvalume /galvanized  -PPGI/PPGL | Hot rolled-cold rolled  - galvanized | Hot rolled-cold rolled  -galvalume /Aluzinc |
| SURFACE  TREATMENT | Mini/regular/big/zero spangle,  Chromate treatment /chromate-free treatment /untreated unoile/oiled,  TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,  Coating,color | Mini/regular/big/zero spangle,  Chromate treatment /chromate-free treatment /untreated unoile/oiled,  TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,  Coating | |
| APPLICATION | Structural use ,roofing, commercial use, household appliance, industry, family | | |
| SPECIAL  APPLICATION | Wear resistant steel, high- strength - steel plate | | |

http://img1.cdn.tradew.com/Y201701M1571336T6G6338831/W0H0/.jpg







http://img1.cdn.tradew.com/Y201701M1571336T6G6338814/W0H0/.jpg



http://img1.cdn.tradew.com/Y201701M1571336T6G6338817/W0H0/.jpg



http://img1.cdn.tradew.com/Y201701M1571336T6G6338821/W0H0/.jpg

