Pe木塑造粒机 PE WPC granulating machine

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 型号Model  | 长径比L/D ratio | 最大产量Max.capacity | 电机功率Motor power  | 适用料Suitable material  | 最大转速Max.rotating speed  | 木粉比例Wood powder percentage |
| SHMS-65 | 40:1 | 200-220kg/h | 75kw | Pe+木粉 wood powder  | 500r/min | ≤75% |
| SHMS-75 | 40:1 | 300-350kg/h | 90kw | Pe+木粉 wood powder  | 500r/min | ≤75% |
| SHMS-90 | 40:1 | 500-600kg/h | 132kw | Pe+木粉 wood powder  | 500r/min | ≤75% |

SHMS系列造粒机用于木塑造粒，与木塑型材生产线为成套设备，造出的颗粒经后经型材生产线挤出制品。该造粒机由平双挤出机、水冷却系统、切粒机、风送冷却系统组成。喂料机与料斗均配有搅拌器，防止原料搭桥。如对颗粒外观无要求，可移除切粒机，直接挤出冷却后进破碎机，可提高生产产量。

SHMS series granulating machine is used for making WPC pellets. The WPC pellets produced by WPC granulating machine can used for making WPC product using WPC machine.The granulating machine consists of parallel double-screw extruder,water cooling system, a granulator and air conveyor cooling system.The feeder and hopper are equipped with mixer to prevent the material blocked up.If customer do not have strict requirements about the appearance of pellets, the granulator can be removed.The pellets extrude by extruder directly, then go for crusher. Can improve the production capacity.