CONCRETE PUMP SINGLE WALL ELBOW

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CONCRETE PUMP SINGEL WALL ELBOW:DN125\*R275\*90D | | | | | | | |
| ID(Inner Diameter) | OD(Outer Diameter) | Thickness(mm) | Bend radius | Collar size | Material | Weight(Kgs) | Service life |
| 125mm | 140mm | 11-12mm | R275 | Sk148mm | Mn13 | 16kgs | 30000 |
| Backend Arc thickness: 14mm |
| CONCRETE PUMP SINGLE WALL ELBOW:DN125\*R275\*45D | | | | | | | |
| ID(Inner Diameter) | OD(Outer Diameter) | Thickness(mm) | Bend radius | Collar size | Material | Weight(Kgs) | Service life |
| 125mm | 140mm | 11-12mm | R275 | Sk148mm | Mn13 | 9kgs | 30000 |
| Backend Arc thickness: 14mm |

CONCRETE PUMP DOUBLE LAYER ELBOW

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CONCRETE PUMP TWIN WALL ELBOW:DN125\*R275\*90D | | | | | | | |
| ID(Inner Diameter) | OD(Outer Diameter) | Thickness(mm) | Bend radius | Collar size | Material | Weight(Kgs) | Service life |
| 125mm | 140mm | Inner elbow thickness:10-11mm | R275 | Sk148mm | Inner elbow :Alloy steel | 16 | 50000cbm |
| Outer elbow thickness:3-4mm | Outer elbow: Q235 |
| Ending collar thickness:7-8mm |
| CONCRETE PUMP TWIN WALL ELBOW:DN125\*R275\*45D | | | | | | | |
| ID(Inner Diameter) | OD(Outer Diameter) | Thickness(mm) | Bend radius | Collar size | Material | Weight(Kgs) | Service life |
| 125mm | 140mm | Inner elbow thickness:10-11mm | R275 | Sk148mm | Inner elbow :Alloy steel | 9 | 50000cbm |
| Outer elbow thickness:3-4mm | Outer elbow: Q235 |
| Ending collar thickness :7-8mm |